## Slide 2
Hashimoto Vacuum Furnace
at the University of Chicago
Experimental conditions:
T=1600˚-1900˚C
P<10-6 Torr

## Slide 4
False color images of two Ca-Al-rich inclusions (CAIs) from the Allende meteorite
Note their igneous texture
CAIs are the oldest known objects to have formed in protostellar disk that became our solar system

## Slide 5
FLUX
Concentration
Distance
FLUX
One can assume that like heat, chemical fluxes are proportional
to concentration gradients
The constant of proportionality is then called an
Effective Binary Diffusion Coefficient: DEBDC.
Chemical Diffusion in Geological Materials

## Slide 6
Chemical Diffusion in molten silicates

## Slide 7
RB-2
15 hours at 1400˚C, 1.0 GPa

## Slide 8
RB-2
15 hours at 1400˚C, 1.0 GPa

## Slide 9
CaO
Al2O3
SiO2
Distance
Molten CAS System
CaO-Al2O3-SiO2

## Slide 10
CaO
Al2O3
SiO2
Distance
Molten CAS System
CaO-Al2O3-SiO2

## Slide 11
CaO
Al2O3
SiO2
Distance
N=3 component system
CaO-Al2O3-SiO2

## Slide 12
CaO
Al2O3
SiO2
Distance
N=3 component system
CaO-Al2O3-SiO2

## Slide 13
CaO
SiO2
Al2O3
mAl2O3
“Incompressibility”
Thermodynamics
High SiO2 Low SiO2
Al2O3 concentration

## Slide 14
RB-2
15 hours at 1400˚C, 1.0 GPa

## Slide 15
RB-2
Evidence that 40Ca
diffuses measurably
faster than 44Ca

## Slide 17
Soret Experiment SRT 4
material: SUNY MORB
DT=170˚C P=1.7GPa
Temperatures determined using
Watson’s spinel thickness method

## Slide 22
Bowen in 1921 argued that thermal fractionation is not relevant
for igneous petrology because and thus temperature
differences will dissipate much to fast for chemistry to respond.
Possible exception: Double-diffusive boundary layers.
For most geological applications

## Slide 23
Basalt Rhyolite
2
0
-2
-4
-6
-8
Typical precision
~ 0.2‰

## Slide 24
RB-2
15 hours at 1400˚C, 1.0 GPa

## Slide 25
RB-5
6 minutes at 1400˚C

## Slide 26
0
-20
-40
d7Li ‰
Li (ppm)
1000
800
400
200
0

## Slide 27
Summary of Key Ideas from Experiments with Silicate liquids:
The constitutive equation for chemical fluxes involves both
a diffusion matrix Dij and a thermal diffusion coefficient DT.
2. When used for isotopes the chemical diffusion coefficients Dij
depend on the isotope mass in such a way that the light isotope
diffuses faster.
3. The thermal diffusion coefficient DT depends on isotope mass
in such a way that the heavier isotope always goes to the cold end.

## Slide 28
Does one find similar kinetic isotope
fractionation by diffusion in natural
settings ?

## Slide 29
Fit using same
b as lab case
Vinal Cove, Vinalhaven Island in
Penobscot Bay, Maine

## Slide 30
Olivine: Mg2SiO4 +Fe2SiO4
(forsterite) (fayalite)

## Slide 32
Olivine: Mg2SiO4 +Fe2SiO4
(forsterite) (fayalite)

## Slide 33
Parkinson et al. (2007)
Clinopyroxene grain from
A lava flow
Western Solomon Is.

## Slide 34
Clinopyroxene grain from a San Carlos zenolith
(Jeffcoate et al., 2007)

## Slide 39
core
overgrowth
overgrowth

## Slide 42
6Li
7Li

## Slide 43
Richter et al. 2013
Flux of Li into the grain
with no concentration
Gradient ?
Coogan et al. (2005) experiment Parkinson et al. (2007) natural sample

## Slide 44
Chart: Log fO2
| -12 | -12 | -17 | -17 | -12 | -12 | -15 | -16 | -12
log D | -9.0362 | -8.7959 | -7.4815 | -7.4318 | -7.9208 | -9.3372 | -11.699
Lof D Coogan | -8.6021 | -9.5

## Slide 45
Chart: Distance mm
| 0 | 7 | 22.297058540778359 | 37.594117081556711 | 52.891175622335062 | 68.188234163113407 | 83.48529270389173 | 98.78235124467011 | 114.0794097854485 | 129.37646832622681 | 144.67352686700519 | 159.97058540778349 | 175.2676439485619 | 190.56470248934019 | 205.8617610301186 | 221.15881957089701 | 236.4558781116753 | 251.75293665245371
Li conc | 2.0002 | 1.7768 | 1.4483 | 1.3095 | 1.0559 | 1.0176 | 1.0116 | 1.0103 | 0.99416 | 1.0108 | 0.95969 | 1.0044 | 0.94394 | 1.0005 | 1.001 | 0.99118 | 1.0031 | 0.99587
Chart: Distance mm
| 7 | 22.297058540778359 | 37.594117081556711 | 52.891175622335062 | 68.188234163113407 | 83.48529270389173 | 98.78235124467011 | 114.0794097854485 | 129.37646832622681 | 144.67352686700519 | 159.97058540778349 | 175.2676439485619 | 190.56470248934019 | 205.8617610301186 | 221.15881957089701 | 236.4558781116753 | 251.75293665245371
del 7Li | -3.229 | -13.386 | -14.098 | -6.897 | -1.691 | 1.461 | -0.186 | 2.145 | -0.23 | 1.539 | 5.053 | -1.55 | -1.135 | -1.294 | -2.627 | 0.408 | -3.316

## Slide 46
Fit using same
b as lab case
Vinal Cove, Vinalhaven Island in
Penobscot Bay, Maine

## Slide 47
Olivine: Mg2SiO4 +Fe2SiO4
(forsterite) (fayalite)

## Slide 49
Kinetic isotope fractionations are an essential
tool for determining the process responsible
for quenched chemical gradients or mineral zoning.
and
Only when the gradients or zoning are shown
to be due to diffusion can they be used to give
a measure of time and cooling rates.
The Overall Punch Line:

## Slide 50
“Here I present experimental data showing that, between and basic and acidic silicate melt,
Isotopic exchange proceeds much more quickly than chemical homogenization.”
Richter F.M. (1993) A method for determining activity-composition relations using chemical
diffusion in silicate melts, Geochim. Cosmochim. Acta 57, 1-14.